## Slide 1: Total Dissolved Solid (TDS)
R & D TEU Division
Last update : 2 June 2025
Sharing Technical

## Slide 2: Outline
R & D TEU Division
Confidential – for Internal use only
Introduction
1
2
3
4
Chemical Recovery
Evaluation of TDS
Conclusion

## Slide 3: Outline
R & D TEU Division
Confidential – for Internal use only
Background
Objective
Total Dissolve Solid (TDS) is key parameters in the kraft recovery cycle, especially before the recovery boiler.
High TDS can cause operational inefficiencies (Impact to LUC).
To provide clear understanding of what TDS & Role in kraft pulp process.
To share actual plant data & trend related to TDS monitoring.
To promote awareness and best practices for optimizing TDS.

## Slide 4: Chemical Recovery Kraft Pulp Cycle
R & D TEU Division
Confidential – for Internal use only
Scope TDS

## Slide 5: Black Liquor Properties
R & D TEU Division
Confidential – for Internal use only
Inorganics
Organics
Liquors Properties in Mill |  |  |  |  |  |  |  |  | 
Area |  | Total Solid | Density |  | Organic Content | Caloric Value | Na | K | CL-
 |  | % | g/cm3 | Temp C | % DB | KCal/Kg (DB) | % DB | % DB | % DB
WBL FL-8 |  | 15.7 | 1.09 | 29.96 | 62.3 | 3333 | 18.74 | 1.59 | 0.56
HBL VE-12 |  | 75.1 | 1.51 | 29.48 | 62.3 | 3325 | 19.89 | 1.96 | 0.64

## Slide 6: Black Liquor Properties
R & D TEU Division
Confidential – for Internal use only
As solid content increases, the viscosity increases sharply.
At higher temperatures, the viscosity is lower for the same solids content
This means heating the BL can help reduce viscosity, which is important for pump to spray gun.
How To Reduction of Viscosity :
By increasing temperature of the liquor. Therefore in any case, strong black liquor temperature is not allowed to go below 90°C to avoid transport & storage problems. Normally 11O°C ~ 120°C is kept for spraying black liquor at recovery furnace.
Decrease of Concentration, Therefore decreasing solid content is not attempted with a view to decrease viscosity.
Increasing residual alkali, Work has already been done to increase the residual alkali of black liquor for hard wood. The data indicate that how residue active alkali decrease the viscosity. It is also suggested that minimum residual active alkaIi to be maintained is 6 gpl. (Ray, Dkk., 1992)

## Slide 7: TDS Flowchart Perawang Mills
R & D TEU Division
Confidential – for Internal use only
Fiberline
WBL Stock
VE Process
HBL Stock
RB Firing
Sampling point
Sampling point
Sampling point
Sampling point
WBL volume | A | 82,194 | m3
Total Solid | B | 14.10 | %
TDS | C | 12,170 | TDS
TDS Ratio | - | 1.35 | TDS/Adt
WBL Feed | D | 25,105 | m3
Total Solid | E | 14.13 | %
TDS | F | 3,717 | TDS
HBL Product | G | 11,168 | m3
Total Solid | H | 76.1 | %
TDS | I | 11,081 | TDS
HBL Firing | J | 13,461 | m3
Temp HBL | K | 132.5 | oC
Total Solid | L | 75.0 | %
TDS | M | 14,703 | TDS
TDS Ratio Wet | N | 1.45 | TDS/Adt Wet Pulp
TDS Ratio HTW | O | 1.45 | TDS/Adt HTW Pulp
C = A * %B * (1+0.0062 * B – 0.0005 * 80)
F = D * %E * (1+0.0062 * E – 0.0005 * 80)
I = G*%H*(1+0.0062*H-0.0005*120)*0.92
M = J*%L*(1+0.0062*L-0.0005*K)*0.92
Pulp Production
9,024 Wet
8,981 HTW
Note :
Density = (1+0.0062*Total Solid(%) – 0.0005*Temperature)
1

## Slide 8: Breakdown Calculation TDS
R & D TEU Division
Confidential – for Internal use only
1. HPD Formula : Flow HBL M3 x TS/100 x density x 0.92 x 24
ρ / SpGr formula : (TS x 6.2 + 1000 – Temperature HBL / 2) / 1000
Constanta 0.92 : Solid 92 % (Ash 8%)
Time Calculation : 24 Hours
TS (%) : Total Solid based on Lab results
Example RB 6 : 11 Dec 2024
Flow HBL : 164 M3/Hr
TS : 73.6%
Temp. HBL : 134.2 oC
Calculate : 164 x (73.6/100) x (73.6 x6.2+1000 – 134.2/2)/1000) x 0.92 x 24
: 164 x (73.6/100) x 1,389 / 1000 x 0.92 x 24 = 3,702 TDS
Remarks :
black liquor density can be determined using total solid (%) and temperature (oC) correlation.
!

## Slide 9: Attachment
R & D TEU Division
Confidential – for Internal use only

## Slide 10: Evaluation of TDS
R & D TEU Division
Confidential – for Internal use only
Parameter | Unit | Jan-24 | Feb-24 | Mar-24 | Apr-24 | May-24 | Jun-24 | Jul-24 | Aug-24 | Sep-24 | Oct-24 | Nov-24 | Dec-24 | Jan-25 | Feb-25 | Mar-25 | 2024 | 2025
Pulp Production | ADT/D | 8,191 | 8,674 | 8,431 | 8,666 | 8,701 | 8,619 | 8,416 | 8,307 | 8,589 | 8,319 | 6,936 | 8,761 | 8,768 | 8,695 | 8,905 | 8,384 | 8,789
Kappa Number | - | 19.2 | 19.2 | 18.5 | 17.8 | 18.0 | 18.0 | 17.8 | 17.8 | 18.3 | 18.5 | 19.1 | 18.9 | 19.1 | 19.0 | 19.4 | 18.4 | 19.1
WL Cooking | Kg/Adt | 306 | 300 | 301 | 312 | 309 | 308 | 304 | 312 | 310 | 306 | 305 | 301 | 298 | 295 | 302 | 306 | 298
WBL Ratio | m³/Adt | 9.39 | 9.35 | 9.40 | 9.43 | 9.28 | 9.14 | 9.22 | 9.21 | 9.34 | 9.14 | 9.52 | 9.12 | 9.05 | 8.96 | 8.98 | 9.3 | 9.0
Total Solid WBL | % | 13.93 | 14.21 | 14.05 | 14.22 | 14.08 | 14.28 | 14.40 | 14.20 | 14.08 | 14.03 | 13.64 | 14.07 | 14.14 | 14.31 | 14.48 | 14.1 | 14.3
Organic TS WBL | % DB | 61.15 | 61.95 | 62.61 | 61.97 | 61.77 | 61.95 | 62.05 | 62.05 | 61.54 | 62.40 | 61.58 | 61.65 | 61.83 | 62.16 |  | 61.9 | 62.0
Total Solid HBL Firing | % | 73.8 | 73.7 | 74.2 | 73.6 | 73.3 | 72.9 | 72.5 | 73.0 | 73.1 | 72.7 | 73.3 | 73.6 | 74.1 | 74.6 | 74.9 | 73.3 | 74.5
Volume WBL to VE | m³/day | 76,919 | 81,135 | 79,181 | 81,709 | 80,700 | 78,721 | 77,448 | 76,774 | 80,167 | 75,985 | 66,574 | 79,872 | 79,273 | 77,862 | 79,923 | 77,932 | 79,019
Volume HBL Firing | m³/day | 13,368 | 14,457 | 13,810 | 14,206 | 13,905 | 14,223 | 14,028 | 13,736 | 14,172 | 13,482 | 11,349 | 14,091 | 14,067 | 13,930 | 14,357 | 13,736 | 14,118
Total Net firing | TDS/D | 12,605 | 13,632 | 13,130 | 13,381 | 13,006 | 13,217 | 12,950 | 12,796 | 13,225 | 12,490 | 10,622 | 13,445 | 13,606 | 13,591 | 14,094 | 12,875 | 13,764
TDS Ratio | TDS/Adt | 1.55 | 1.57 | 1.55 | 1.55 | 1.51 | 1.53 | 1.54 | 1.54 | 1.53 | 1.50 | 1.55 | 1.54 | 1.55 | 1.57 | 1.58 | 1.54 | 1.57
Steam Production | Ton | 41,114 | 43,858 | 42,464 | 43,810 | 43,101 | 43,773 | 42,878 | 41,945 | 43,848 | 41,725 | 35,400 | 44,272 | 43,564 | 42,615 | 43,853 | 42,349 | 43,344
Steam Ratio | Ton/TDS | 3.26 | 3.22 | 3.23 | 3.27 | 3.31 | 3.31 | 3.31 | 3.28 | 3.31 | 3.34 | 3.35 | 3.34 | 3.26 | 3.19 | 3.17 | 3.29 | 3.21

## Slide 11: Evaluation of TDS - Blow Line Kappa , WL Oxidation consumption and TDS
R & D TEU Division
Confidential – for Internal use only
Chart: TDS/Adt
| Jan-24 | Feb-24 | Mar-24 | Apr-24 | May-24 | Jun-24 | Jul-24 | Aug-24 | Sep-24 | Oct-24 | Nov-24 | Dec-24 | Jan-25 | Feb-25 | Mar-25
RB Total TDS | 1.55 | 1.5663 | 1.5474 | 1.5455 | 1.5136 | 1.5286 | 1.5357 | 1.5428 | 1.5331 | 1.5032 | 1.5458 | 1.5376 | 1.5501 | 1.5662 | 1.58
WL Cooking Consumption | 305.6633 | 300.4842 | 300.7127 | 312.066 | 309.1462 | 307.8818 | 304.3178 | 311.6791 | 310.2266 | 305.8994 | 305.4431 | 301.0453 | 298.4522 | 295.0085 | 302
Chart: Kappa Number
| Jan-24 | Feb-24 | Mar-24 | Apr-24 | May-24 | Jun-24 | Jul-24 | Aug-24 | Sep-24 | Oct-24 | Nov-24 | Dec-24 | Jan-25 | Feb-25 | Mar-25
Kappa Blowline | 19.1984 | 19.2032 | 18.4549 | 17.784 | 18.0345 | 18.0473 | 17.8402 | 17.8345 | 18.3418 | 18.522 | 19.0788 | 18.8985 | 19.0527 | 18.9626 | 19.4
WL Cooking Consumption | 305.6633 | 300.4842 | 300.7127 | 312.066 | 309.1462 | 307.8818 | 304.3178 | 311.6791 | 310.2266 | 305.8994 | 305.4431 | 301.0453 | 298.4522 | 295.0085 | 302
Higher Kappa number reduce WL cooking consumption.

## Slide 12: Evaluation of TDS - Pulp Production , TDS & WBL To Ve
R & D TEU Division
Confidential – for Internal use only
Chart: TDS/ADt
| Jan-24 | Feb-24 | Mar-24 | Apr-24 | May-24 | Jun-24 | Jul-24 | Aug-24 | Sep-24 | Oct-24 | Nov-24 | Dec-24 | Jan-25 | Feb-25 | Mar-25
RB Total TDS | 1.55 | 1.5663 | 1.5474 | 1.5455 | 1.5136 | 1.5286 | 1.5357 | 1.5428 | 1.5331 | 1.5032 | 1.5458 | 1.5376 | 1.5501 | 1.5662 | 1.58
WBL Total Solid | 13.9338 | 14.2089 | 14.0531 | 14.2204 | 14.0815 | 14.2767 | 14.4006 | 14.1975 | 14.0815 | 14.0263 | 13.6378 | 14.0689 | 14.1429 | 14.3054 | 14.48
Chart: Adt
| Jan-24 | Feb-24 | Mar-24 | Apr-24 | May-24 | Jun-24 | Jul-24 | Aug-24 | Sep-24 | Oct-24 | Nov-24 | Dec-24 | Jan-25 | Feb-25 | Mar-25
Pulp Production | 8191.4552 | 8674.4254 | 8430.7937 | 8666.3736 | 8701.01 | 8619.2527 | 8416.0603 | 8307.1222 | 8588.6146 | 8319.4114 | 6936.2958 | 8761.0526 | 8767.6263 | 8695.445 | 8905
WBL Total Solid | 92397.7819 | 95691.041 | 93896.8514 | 97075.7571 | 95723.5647 | 95115.2685 | 94538.515 | 94266.2457 | 95818.3564 | 89005.5871 | 77342.7123 | 91866.5584 | 89933.7774 | 89849.1408 | 91724
WBL Total Solid Increase start Jan 25 From 14.07 to 14.48 %, impacted to TDS Ratio.

## Slide 13: Evaluation of TDS - Pulp Production , TDS & HBL
R & D TEU Division
Confidential – for Internal use only
Chart: TDS/Adt
| Jan-24 | Feb-24 | Mar-24 | Apr-24 | May-24 | Jun-24 | Jul-24 | Aug-24 | Sep-24 | Oct-24 | Nov-24 | Dec-24 | Jan-25 | Feb-25 | Mar-25
RB Total TDS | 1.55 | 1.5663 | 1.5474 | 1.5455 | 1.5136 | 1.5286 | 1.5357 | 1.5428 | 1.5331 | 1.5032 | 1.5458 | 1.5376 | 1.5501 | 1.5662 | 1.58
TS HBL Firing | 73.7524 | 73.7452 | 74.1849 | 73.6403 | 73.2528 | 72.8826 | 72.5275 | 72.9999 | 73.1192 | 72.6692 | 73.3408 | 73.5772 | 74.1428 | 74.5759 | 74.9
HBL Firing Total Solid Increase start Jan 25 From 73.6 to 74.9 %, impacted to increase TDS Ratio.
Chart: TDS/Adt
| Jan-24 | Feb-24 | Mar-24 | Apr-24 | May-24 | Jun-24 | Jul-24 | Aug-24 | Sep-24 | Oct-24 | Nov-24 | Dec-24 | Jan-25 | Feb-25 | Mar-25
TDS RB | 1.55 | 1.5663 | 1.5474 | 1.5455 | 1.5136 | 1.5286 | 1.5357 | 1.5428 | 1.5331 | 1.5032 | 1.5458 | 1.5376 | 1.5501 | 1.5662 | 1.58
Volume HBL firing | 557.0114 | 602.3921 | 575.4048 | 591.9289 | 579.3865 | 592.6069 | 584.5126 | 572.3453 | 590.484 | 561.7422 | 472.8651 | 587.1413 | 586.1444 | 580.4233 | 598.2

## Slide 14: Evaluation of TDS - TDS & Organic Content in TS WBL
R & D TEU Division
Confidential – for Internal use only
Organic content in TS WBL increase Dec 24 – Feb 25.
Increase Total Solid WBL start Jan – Mar 25, 14.1 to 14.5 %
Chart: TDS/Adt
| 45292 | 45323 | 45352 | 45383 | 45413 | 45444 | 45474 | 45505 | 45536 | 45566 | 45597 | 45627 | 45658 | 45689
TDS RB | 1.55 | 1.57 | 1.55 | 1.55 | 1.51 | 1.53 | 1.54 | 1.54 | 1.53 | 1.5 | 1.55 | 1.54 | 1.55 | 1.57
Organic Content in TS | 61.1459 | 61.95 | 62.6106 | 61.9744 | 61.7667 | 61.9475 | 62.049 | 62.0477 | 61.5406 | 62.3981 | 61.5794 | 61.6494 | 61.8259 | 62.1575
Chart: TDS/ADt
| Jan-24 | Feb-24 | Mar-24 | Apr-24 | May-24 | Jun-24 | Jul-24 | Aug-24 | Sep-24 | Oct-24 | Nov-24 | Dec-24 | Jan-25 | Feb-25 | Mar-25
RB Total TDS | 1.55 | 1.5663 | 1.5474 | 1.5455 | 1.5136 | 1.5286 | 1.5357 | 1.5428 | 1.5331 | 1.5032 | 1.5458 | 1.5376 | 1.5501 | 1.5662 | 1.58
WBL Total Solid | 13.9338 | 14.2089 | 14.0531 | 14.2204 | 14.0815 | 14.2767 | 14.4006 | 14.1975 | 14.0815 | 14.0263 | 13.6378 | 14.0689 | 14.1429 | 14.3054 | 14.48

## Slide 15: Attachment
R & D TEU Division
Confidential – for Internal use only

## Slide 16: Formula TDS Perawang Mills
R & D TEU Division
Confidential – for Internal use only
Area | Item | Nota | Unit | Remark
FL | Prod Wet Pulp | A | Adt | Totalizer on 06:00
 | Prod HTW | A1 | Adt | Totalizer on 06:00
 | Blow Line Kappa | - | - | Lab Testing - Avg weighted
 | WL Cooking | - | kg/adt | Totalizer Avg FL+RC - Cal
 | WBL to VE, FL | B | m³ | Totalizer on 06:00
 | WBL Ratio | C | m³/Adt | C = B / A
 | TS WBL to VE,FL | D | % | Lab Testing - Avg weighted
 | TDS Sent to VE, FL | E | TDS | E = B * %D * (1 + 0.0062*D - 0.0005*80)
 | TDS Ratio - FL | F | TDS/Adt | F = E / A
VE | Volume WBL Stock, VE | G | m³ | Tank Level - 06:30
 |  | H | Δ Stock | H = Gtoday - GY'day
 | TDS in WBL Stock VE | I | TDS | I = G * %K * (1 + 0.0062*K - 0.0005*80)
 | Volume WBL Feed VE | J | m³ | Totalizer on 06:00
 | TS WBL Feed VE | K | % | Lab Testing - Avg weighted
 | TDS in WBL Feed to VE | L | TDS | L = J * %K * (1 + 0.0062*K - 0.0005*80)
 | Volume HBL Stock at VE | M | m³ | Tank Level - 06:30
 | TS HBL at VE | N | % | Lab Testing - Avg weighted
 | TDS in HBL Stock at VE | O | TDS | O = M * %N * (1 + 0.0062*N - 0.0005*120) * 0.92
 |  | P | Δ Stock | P = Otoday - OY'day
 | HBL Production | Q | m³ | Q = P + U
 | TDS Production VE | R | TDS | R = Q * %N * (1 + 0.0062*N - 0.0005*120) * 0.92
 | Ratio WBL to HBL | S | m³/m³ | S = J / Q
RB | Total TDS Production | T | TDS | Reff. to Sheet TDS Cal;Row 63
 | Volume HBL Firing | U | m³ | Reff. to Sheet TDS Cal;Row 62
 | Temperature HBL Firing | - | °C | Reff. to Sheet TDS Cal;Row 90
 | TS HBL Firing | - | % | Reff. to Sheet TDS Cal;Row 89
 | TDS HBL Firing | V | TDS | Reff. to Sheet TDS Cal;Row 56
 | TDS Ratio Wet Pulp | W | TDS/Adt | W = T / A
 | TDS Ratio HTW | AA | TDS/Adt | W = T / A1